High Temperature Radiation Hard Devices Based on SiC

E. Kalinina, N. Strokan, A. Ivanov, А. Strel’chuk, A. Lebedev

Ioffe Physical-Technical Institute of  the Russian Academy of Sciences, 26 Politechnicheskaya str., 194021 St.Petersburg, Russia

evk@mail.ioffe.ru

Modern development of the atomic industry, nuclear energy, military and cosmic technique are urgently required in development of the new electronics generation capable of operating under extreme conditions, i.e., at high temperatures, at high radiation levels and in chemically active environments. Up to now such devices could not be fabricated with conventional semiconductor materials like Ge, Si, CdTe or GaAs. The wide band gap semiconductor SiC is the most perspective material for these purposes due to the high value of threshold energy for defect production as well as the excellent chemical, electrical and mechanical properties.

The purpose of this work was both the study of the electro-physical properties of initial SiC material before and after irradiation as well as the development of radiation hardness high temperature devices and detectors based on it.

The pure epitaxial layers 4Н and 6Н-SiC, diode and transistor structures were irradiated with protons (8 MeV), electrons (900 keV), neutrons (1 MeV), gamma-ray photons, high power pulsed X-ray radiation [3х1010 rd(SiC)/s] as well Kr (245 МeV) and  Bi (710 МeV) ions. The spectrometry of short range ions was produced using -particles (4.8 - 7.7 МeV) formed during the natural decay.

The main results are as follows:

- For the first time the considerable improvement of the charge collection efficiency and the energy resolution with rising temperature up to 4000С of  SiC detectors and matrix with its was experimental shown.

- For the first time the energy resolution of  0.34 % (18.8 кэВ), commensurable with best Si-detectors, has been achieved for using SiC structures with Schottky barriers.

-  It was revealed for the first time, that diodes degraded after irradiation with fast neutrons and high-energy Kr and Bi ions, when SiC epitaxial layers changed into dielectric, recovered their rectifying properties at the temperature up to 500oC. Consequently, the radiation resource and lifetime of devices based on SiC could be considerably increased under high working temperatures.

- For the first time the transistor structure SiC based detectors were realized with the signal amplification by a factor of tens under irradiation with protons. This internal amplification of the signal held good for protons with dose of 5x1013 см-2 corresponding to the relativistic protons dose of 5x1015 см-2   that is of interest to the high energy physics.

-  The kinetics of SiC power diode structures was studied under 22 ns ionization pulse X-ray radiation in the dose rate range up to 3x1010 rd(SiC)/s. The diode recovery time was determined to be equal to 25 ns, that indicats the hardness of SiC devices to the high dose rate effects.

-  The damage structure formation in SiC is independent on the processes determined by the ionizing energy losses by ionization in the tracks of heavy high energy ions up to level of 34 keV/nm and is governed by  radiation damage produced as a result of elastic-collision events.