Feasibility study of the use of radiogenic lead as a coolant of nuclear reactors

A.N. Shmelev1), G.G. Kulikov1,2), V.A. Apse1), V.V. Artisyuk3)

1) Moscow Engineering Physics Institute (State University), Kashirskoe shosse 31, Russia

Tel: +7-(495)-323-92-42, Email: shmelan@mail.ru

2) International Science and Technology Center (ISTC), Krasnoproletarskaya ulitsa 32-34, Moscow, Russia, Tel: +7-(495)-982-31-54, Email: kulikov@istc.ru

3) Obninsk State Technical University of Nuclear Power Engineering, Russia

Radiogenic lead is a final product of radioactive decay chains in uranium and thorium ores. After a number of alpha- and beta-decays, the starting isotopes 232Th, 238U and 235U are converted into stable lead isotopes: 208Pb, 206Pb and 207Pb, respectively. Radiogenic lead with a large fraction of 208Pb has unique neutron-physical properties because 208Pb is a double magic nuclide with closed proton and neutron shells in nucleus. That is why 208Pb has an extremely low cross-section of thermal neutron capture reaction (~0.5 mb) in comparison with common lead (~175 mb) and graphite (~3.5 mb) (see Fig.1).

| Fig.1. Neutron capture cross-sections of natural lead, Pb-208 isotope and graphite. | Fig.2. The excitation levels of lead nuclides. |
| --- | --- |

In addition, 208Pb is a weak neutron moderator through inelastic scattering of fast neutrons owing to the higher first energy excitation level of nucleus (~2.6 MeV for 208Pb as against ~0.6-0.9 MeV for common lead, see Fig.2) and through elastic scattering owing to a high atomic number. So, high 208Pb content in lead coolant of fast reactor allows a decrease in the unfavorable spectral component in a coolant temperature reactivity coefficient [1].

In spite of 208Pb content being as high as 52% in common lead, the remaining lead fraction (mainly 207Pb and 204Pb isotopes) is characterized both by a large neutron capture cross-section and essential inelastic scattering. Radiogenic lead from thorium and uranium-thorium ores has a very low fraction of these unfavorable isotopes.

The use of radiogenic lead as a coolant and graphite as a structural material creates favorable conditions for development of high-temperature and high-flux reactors. Such a high-temperature reactor differs profitably from He-cooled HTGR by low pressure and natural circulation of coolant, while such a high-flux reactor makes it possible to transmute radioactive isotopes with extremely low neutron capture cross-sections, like 90Sr and 137Cs.

Plutonium in (238U-Pu-Th-233U)-fuel could be proliferation-protected at an isotopic level by creating favorable conditions for intense generation of even Pu-isotopes. These conditions could be created if radiogenic lead is used as a coolant and graphite – as a structural material and neutron moderator. In this case, transition from hard to softened neutron spectrum results in substantial worsening of 239Pu neutron capture properties while those of 233U undergo quite insignificant changes. In addition, Pu proliferation protection at an isotopic level is provided under high rate of secondary fuel breeding (mainly of 233U) just due to weak neutron absorption by radiogenic lead and graphite.

Publications on large deposits of thorium and uranium ores [2-6] (see Table 1) show that radiogenic lead mainly consists of 208Pb (useful isotope with low cross-sections of neutron capture). If necessary, 208Pb may be extracted from already available tailing stocks of uranium and uranium-thorium ore processing mills as a by-product.

Table 1

Main Deposits of Uranium, Thorium and Mixed Uranium-Thorium Ores. Elemental Compositions of Minerals and Isotope Compositions of Radiogenic Lead

| Deposit | U / Th / Pb, wt.% in mineral | Pb isotopes, atomic % ( 204 / 206 / 207 / 208 ) |
| --- | --- | --- |
| Brazil, Black Sands Beach, Guarapari, Espirito Santo state, monazite [2] | 1.26/59.3/1.51 | 0.005/6.030/0.455/93.51 |
| Brazil, Buena, Rio de Janeiro state, monazite [2] | 1.72/45.1/1.24 | 0.030/11.10/1.09/87.783 |
| Canada, Manitoba, monazite [3] | 0.28/15.63/1.52 | 0.0097/10.20/1.86/87.93 |
| Australia, Mt. Isa Mine, monazite [3] | 0.0/5.73/0.285 | 0.038/5.44/0.972/93.55 |
| India, Singar Mine, uraninite [4] | 64.3/8.12/8.92 | 0.0/89.38/6.44/4.183 |
| India, Gaya district, monazite [5] | 0.49/10.55/0.23 | — |
| USA, Las Vegas, New Mexico, monazite [3] | 0.122/9.39/0.37 | 0.025/9.068/1.127/89.78 |
| Ukraine, River South Byug, monazite [6] | 0.18/8.72/0.91 | 0.01/6.04/0.94/93.0 |
| «Common» lead | – | 1.4/24.1/22.1/52.4 |

So, radiogenic lead as a coolant of power nuclear reactors can improve their operation safety, provide proliferation protection of fissionable materials and intensify fuel breeding. In addition to energy generation, radiogenic lead-cooled reactors could be used for hydrogen production and some other kinds of artificial fuel, for production of high-temperature heat and for effective transmutation of radioactive isotopes with extremely low cross-sections of neutron capture reaction. Radiogenic lead opens new opportunities for improving the neutron-physical parameters of nuclear reactors and for widening the areas of their future application.

References

- A.N. Shmelev, et al. Radiowaste Transmutation in Nuclear Reactors. Proceedings of a Specialist Meeting “Use of Fast Reactors for Actinide Transmutation”, September 22-24, 1992, Obninsk, Russia, IAEA-TECHDOC-693, IAEA, pp.77-86, March 1993.

- Jose Marcus Godoy, et al. Aronne. Application of Inductively Coupled Plasma Quadrupole Mass Spectrometry for the Determination of Monazite Ages by Lead Isotope Ratios. – Journal of Brazilian Chemical Society, Vol.18, No.5, Sao Paulo, 2007.

- A.O. Nier, et al. The Isotopic Constitution of Lead and the Measurement of Geological Time. – Physical Review, Vol.60, July 15, pp.112–117, 1941.

- A. Holmes, “The Pre-Cambrian and Associated Rocks of the District of Mozambique,” Quarterly Journal of Geological Society, Vol.74, pp.31-98, 1918.

- T. C. Sarkar, “The Lead Ratio of a Crystal of Monazite from the Gaya District, Bihar,” Proceedings of Indian Academy of Sciences, Vol.13, pp.245-248, 1941.

- Catalog of Isotope Dates for Minerals of Ukrainian Shield, pp.90-91 and pp.136-137, Naukova Dumka, Kiev, (in Russian), 1978.