NITI severe accident research under ISTC coordination

V.A. Vasilenko, V.B. Khabensky, S.V. Bechta*, V.S. Granovsky

Alexandrov Research Institute of Technology (NITI), Sosnovy Bor, Russia

* Corresponding author, Tel: +7 81369 22064, Fax:+7 81369 23672, E-mail: rital@sbor.net

Abstract

From the very start of ISTC activities NITI has been involved in its projects on the conversion of industrial and engineering potential from military to civil needs and priorities. These projects include studies aimed at efficient severe accident management (SAM) and safety enhancement of commercial nuclear reactors. Detailed information on the projects is published in /1 - 11/.

Most of the experimental studies have been carried out in the RASPLAV experimental platform, which:

- Comprises 4 experimental facilities integrated into the shared infrastructure of auxiliary and protective systems. The experimental facilities are based on the principle of induction melting in a cold crucible (IMCC) at different heating frequencies;

- Enables melting and various manipulations with chemically prototypic corium having mass up to 8 kg and temperature up to 3200 С in different atmospheres (inert (Ar, He), oxidizing (steam, air), or their mixtures);

- Is certified for work with unirradiated uranium and radiolabeled fission product simulants.

In the EU countries results of these ISTC projects are used for reactor application particularly for optimization of NUCLEA - European thermodynamic database, development and implementation of different SAM concepts. Results delivered by the ISTC projects together with data of other projects carried out within national programs have an important reactor application in Russia, i.e.:

- Jointly with SPbAEP ex-vessel SAM concept [12] has been developed, which foresees corium retention in the reactor cavity of Tyanvan NPP (China) and Kudankulam NPP (India) equipped by VVER-1000 reactors.

- New oxidic sacrificial material [13] has been developed jointly with ISCh RAS and RSC KI. This material is a key component in the above-mentioned melt retention concept.

- New crucible-type core catcher for VVER-1000 [14] has been developed and justified in collaboration with SPbAEP, RRC KI, IBRAE RAS, PKF of ROSENERGOATOM, ISCh RAS, SPbGETU, IPPE and SPb GTI (TU).

- Concept of in-vessel corium retention has been justified for VVER-640 project based on the application of passive safety systems.

The developed concept, ex-vessel catcher and innovative solutions are currently in use in the NPP-2006 projects with VVER-1200, which are under construction in Russia.

Long-term and diverse experience in international projects coordinated by the ISTC generated fruitful cooperation on severe accident issues between NITI and European organizations. The following formats of cooperation can be mentioned:

- Multi-lateral exchanges with European scientific research centers collaborating within the ISTC projects.

- Multi-lateral cooperation coordinated by the OECD and RSC KI with the participants of MASCA program. NITI took part in preparing CORTRAN program proposal.

- Bilateral cooperation within the ISTC partnership projects.

- Bilateral cooperation with CEA coordinated by Rosatom.

- Communication with SARNET, so far unilateral (SARNET members have an access to the ISTC project results through the CEG-SAM website).

Short-term perspectives of a broader cooperation are related to the NITI’s initiative to participate in:

- ROSATOM-EUROATOM program. In particular, a joint call on containment phenomena is under preparation for transnational use of large scale experimental facilities: MISTRA, CEA – PANDA, PSI – KMS, NITI

- SARNET network of excellence, i.e. in the packages related to severe accident research.

References

- Yu.B. Petrov, D.B. Lopukh, S.V. Bechta, al., Corrosive capacity of superheated corium melt. Advanced materials. 3 (1996) p.374-378

- S. V. Bechta, V. B. Khabensky, S. A. Vitol, et al. Corrosion of vessel steel during its interaction with molten corium. Part 1: Experimental, J. Nucl. Eng. Design, 236, pp. 1810-1829 (2006).

- S. V. Bechta, V. B. Khabensky, S. A. Vitol, et al. Corrosion of vessel steel during its interaction with molten corium. Part 2: Model development, J. Nucl. Eng. Design, 236, pp. 1362-1370 (2006).

- S.V. Bechta, V.S. Granovsky, V.B. Khabensky, et al. Corium Phase Equilibria based on MASCA, METCOR and CORPHAD Results, Nuclear Engineering and Design 238, pp. 2761-2771 (2008).

- S.V. Bechta, V.S. Granovsky, V.B. Khabensky, et al. VVER Vessel Steel Corrosion at Interaction with Molten Corium in Oxidizing Atmosphere, Nuclear Engineering and Design, in Press, Corrected Proof, http://dx.doi.org/10.1016/j.nucengdes.2008.12.009.

- Bechta S.V., Krushinov E.V., Almjashev V.I., et al. Phase diagram of the ZrO2–FeO system. J. Nucl. Mater. V 348. N 1–2. P. 114–121. (2006).

- Bechta S.V., Krushinov E.V., Almjashev V.I., et al. Phase relations in the ZrO2–FeO system. Rus. J. Inorg. Chem. V. 51. N. 2. P. 325–331. (2006).

- L.P. Mezentseva, S.V. Beshta, V.B. Khabensky, et al. Phase and Chemical transformations in the SiO2–Fe2O3(Fe3O4) system at various oxygen partial pressures. Russian J. Inorgan. Chem. V. 51. N 1. P. 118–125. (2006).

- S.V. Bechta, E.V. Krushinov, V.I. Al’mjashev, et al. Phase transformation in the binary section of the UO2-FeO-Fe. Radiochemistry. V. 49. N 1. P. 20–24. (2007).

- Bechta S.V., Krushinov E.V., Almjashev V.I., et al. Phase diagram of the UO2–FeO1+x system. J. Nucl. Mater. V. 362. N 1. P. 46–52. (2007).

- S.V. Bechta, E.V. Krushinov, S.A. Vitol, et al. Influence of corium oxidation on fission product release from molten pool. Proc. of ICAPP ‘09, Tokyo, Japan, May 10-14, Paper 9145 (2009).

- I.V. Kukhtevich, V.V. Bezlepkin, V.S. Granovskii et al. The Concept of Localization of the Corium Melt in the Ex-vessel Stage of a Severe Accident at a Nuclear Power Station with a VVER-1000 Reactor. Thermal Engineering, 2001, vol. 48, № 9, p.699-707

- V.V. Gusarov, V.I. Al’myashev, S.V. Bechta et al. Sacrificial Materials for Safety Systems of Nuclear Power Stations: A New Class of Functional Materials. Thermal Engineering, 48, 9, 721, (2001)

- V.G. Asmolov, S.V. Bechta, V.M. Berkovich et al. Crucible-type Core Catcher for VVER-1000 Reactor. Proc. of ICAPP05 Seoul, Korea, May 15-19, 2005, Paper 5328